## Slide 1
Assessment of Pipeline Buried Valves
CONFERENCE
ORGANIZERS

## Slide 2: Assessment of Pipelines Buried Valves
Mohanned Tarabzouni | Aramco

## Slide 3: Background
Aramco Pipeline System Network
Services, Temperaure And Pressure
Inspection and Maintenance
+30,000 KM in length
Size range from 8-60 inches
Sour/Sweet, NGL, Crude, Gas and refined products
Complex geometry and elevation changes
40-60 yrs in service
Inline inspection + pigging
10,000+ valves

## Slide 4: Design Specs
Multiple buried pipelines
FBE Coated
Tape Wrapped
Buried valves with same coating
30+ years of service
Multiple soil, weather and environment changes
Not commonly inspected

## Slide 5: Challenges
Coating condition and design life
Cathodic protection continuity and effectivness
Valve body material and coating selection
Difficulties to periodic inspection

## Slide 6: Challenges
Coating condition and design life
Cathodic protection continuity and effectivness
Valve body material and coating selection
Difficulties to periodic inspection

## Slide 7: Case Study 1
56 inch top entry ball valve
Fully buried
FBE coated
Gas over oil operated
Minor gas release due to loose bonnet bolts

## Slide 8: Analysis
Improperly torqued bonnet bolts
Difficult (not feasilbe) to be removed since its welded to pipeline
Possible bonnet gasket/seal damage

## Slide 9: Recommendations
Includes coating, cathodic protection, material selection and environmental assessment/impact
Proper inspection program based on severity, location and other factors impacting the valve’s performance

## Slide 10: Case Study 2
40 inch top entry ball valve
FBE coated
Fully buried
Axuliaries failure

## Slide 11: Analysis
Potential external corrosion failure
Shield cathodic protection due to multiple connections/joints (union, elbows, coupling)
Coating application condition and procedure not verified
Carbon steel material selected
Threaded without sealwelding
CONFERENCE ORGANIZERS

## Slide 12: Recommendations
Inspect coating condition and develop action plan (Condition vs. Method)
Verify cathodic protection continuity and efficiency along valve an auxiliaries
Includes coating, cathodic protection, material selection and environmental assessment/impact
Proper inspection program based on severity, location and other factors impacting the valve’s performance

## Slide 13: Take Away Notes Thorough review is required to ensure all protection methods Includes coating, cathodic protection, material selection and environmental assessment/impact Proper inspection program based on severity, location and other factors impacting the valve’s performance Corrosion protection/mitigation methods suitable for pipeline valves in addition to associated auxilaries
CONFERENCE ORGANIZERS
ORGANIZERS

## Slide 14
Thank You
Mohanned.Tarabzouni@aramco.com

## Slide 15
ORGANIZING SECRETARIAT
Ph. +39 035 3230904
e-mail info@industrialvalvesummit.com
www.industrialvalvesummit.com
CONFERENCE ORGANIZERS
Ph. +39 3474908420
e-mail segreteria@valvecampus.com
www.valvecampus.com
Thanks