## Slide 1
Corrosion performances and qualification challenges of alloy 625 produced by different additive manufacturing technologies
CONFERENCE
ORGANIZERS

## Slide 2: Corrosion performances and qualification challenges of alloy 625 produced by different additive manufacturing technologies
The pathway through AM alloys qualification
Sergio Lorenzi | Professor

## Slide 3: AIM
Evaluate the role of macro/microstructural features and defects on the corrosion behaviour - localised and selective - of AM Alloy 625.
Compare the performances of wrought and well established AM materials manufactured by L-PBF and DED in the light of the emerging ones based on metal/polymer systems i.e. Mex and BJ

## Slide 4: Alloy 625
Excellent combination of mechanical properties and corrosion resistance in several aggressive environments
Adopted in high added value industrial fields with medium to small lot productions (e.g. aerospace, chemical, oil & gas)
C | Si | Mn | P | S | Cr | Mo | Ni | Nb | Ti | Al | Fe | Nb+Ta | Cu
0.036 | 0.25 | 0.19 | 0.007 |  | 21.6 | 8.26 | 61.92 | 3.660 | 0.243 | 0.199 | 3.11 | 3.67 | -

## Slide 5: Alloy 625

## Slide 6: AM materials and qualification
Standards
Certification
Materials qualification
Mechanical, physical
Corrosion
According to?
…in 2016

## Slide 7: AM materials and qualification
API-20s
TR21522
Corrosion Testing for Additive Manufacturing

## Slide 8: AM corrosion, microstructure and technology related challenges
Process parameters/technologies and corrosion:
  Non-equilibrium microstructures
  Surface finishing (as-build, defects, shot peening, polishing, etching ecc.)
  Porosities
  Residual stresses
  Oxides, segregations
G. Sander, J. Tan, P. Balan, O. Gharbi, D.R. Feenstra, L. Singer, S. Thomas, R.G. Kelly, J.R. Scully and N. Birbilis, Corrosion of Additively Manufactured Alloys: A Review, Corrosion (2018)

## Slide 9: Metal AM
Atomic Diffusion Additive Manufacturing (MFFF, BJ)
Laser Powder Bed Fusion
(LPBF, EBM)
Direct Energy Deposition
(DED)

## Slide 10: Composition - Alloy 625
Elemento (%) | C | Si | Mn | P | S | Cr | Mo | Ni | Nb | Ti | Al | Co | Ta | Fe
L-PBF powder | 0.01 | 0.08 | 0.03 | <0.001 | 0.002 | 22.4 | 8.2 | Bal. | 3.73 | 0.18 | <0.01 | 0.17 | 0.13 | 0.45
DED wire | 0.01 | 0.07 | 0.01 | 0.003 | <0.001 | 22.31 | 9.03 | Bal. | 3.47 | 0.22 | 0.10 | 0.01 | 0.01 | 0.19
MFFF specimen | 0.08 | 0.52 | 0.40 | 0.006 | 0.004 | 19.55 | 8.57 | Bal. | 3.28 | 0.022 | <0.001 | 0.047 | - | 2.61
HW | 0.036 | 0.25 | 0.19 | 0.007 | 0.0010 | 21.60 | 8.26 | Bal. | 3.660 | 0.243 | 0.199 | 0.020 | 0.010 | 3.11
ASTM B443 | Max 0.1 | Max 0.5 | Max 0.5 | - | - | 20-23 | 8-10 | Bal. | 3.15-4.15 | Max 0.4 | Max 0.4 | Max 1 | - | Max 5

## Slide 11: Specimens
Cylinder, 15 mm diameter, 5 mm height
Cubic, 15 mm
L-PBF
DED
Hight 124 mm
Length 230 mm
Thickness 5 mm
70 cm3/h
10 cm3/h
10 cm3/h
MFFF
Corrosion tests
ASTM G5
0.6M NaCl, ph 7 and 3
IGC, ASTM G28

## Slide 12: Microstructure… …and properties
Chart: HV1
| LPBF | DED | MEx | BJ | Hot worked
Serie 1 | 300 | 245 | 200 | 180 | 230
50 µm
50 µm
50 µm
50 µm
50 µm

## Slide 13
«Unique microstructure»

## Slide 14: Macroporosities (technology related defects)

## Slide 15: Macroporosities (technology related defects)
 | LPBF | DED | MEX
Porosity (%) | 0.06 | 0.06 | 3.04
Pores > 50 µm (%) | 0 | 0.02 | 0.37
CORE
layer ± 45°
CONTOUR
Building
direction
CONTOUR
CORE
7,7%
1,3%

## Slide 16: Microporosity
LPBF
DED
MFFF
Specimens | LPBF | Mex | DED
Diameter, mean value [μm] | 2,37 | 4,42 | 2,34
Microporosity | 0,07% | 1,07% | 0,07%

## Slide 17: Corrosion behaviour
10 mV/min scan rate
Deaerated solution (nitrogen)

## Slide 18: Corrosion behaviour
7
10 mV/min scan rate
Deaerated solution (nitrogen)

## Slide 19: Corrosion behaviour
10 mV/min scan rate
Deaerated solution (nitrogen)

## Slide 20
Micro-CT reconstruction
Total porosity: 3.54%

## Slide 21
Corrosion behaviour – IGC tests
LPBF
DED
ADAM
HOT WORKED
ASTM G28
Mex
DED
HOT WORKED
LPBF

## Slide 22
ASTM G28 - method A
IGC tests
50% suphuric acid, 25 ferric sulphate
Metal systems
Metal + polymer systems
Conventional

## Slide 23: Hot worked
100 µm
Cross-section, after G28-A
100 µm
20 µm
Twinning
Mo-, Nb-rich carbides

## Slide 24
CORE
CONTOUR
Mo-, Nb- e Si rich precipitates
Mex

## Slide 25
Microstructure

## Slide 26: BJ
Twinning
2nd phase
Pores
200 µm
Ni
Cr
Mo
Nb
C
Second phase at grain boundaries is enriched in Mo, Nb and C
Ni(γ)
MC-type carbide (NbC)
High porosity (1.70%)

## Slide 27: Conclusions
The experimental work studied AM-Alloy 625 manufactured with 4 different technology to highlight the relevant qualification challenges of a strategic alloy for Oil&Gas industry
Corrosion tests have been performed in order to study the effect of unique macrostructure and microstructure of the material –strictly related to the specific AM technology- on the corrosion performance of the alloy
All the evaluations performed allowed to establish a connection between the different AM technologies adopted and the corrosion behavior of the material, which proved to be very different according to the considered additive manufacturing technology.

## Slide 28: Considerations
AM alloys are for sure «new materials» as the performances – of course mechanical but also corrosion, open the need of specific in depth study to qualify and certify the use in strategic industrial districts
Standardisation is moving fast in a lot of industrial districts and it is a key factor for opening the market of AM metals in relevant industrila sectors such as O&G and Energy (alternative fuels)
From corrosion enginering back to the corrosion science!

## Slide 29
ORGANIZING SECRETARIAT
Ph. +39 035 3230904
e-mail info@industrialvalvesummit.com
www.industrialvalvesummit.com
CONFERENCE ORGANIZERS
Ph. +39 3474908420
e-mail segreteria@valvecampus.com
www.valvecampus.com
Thanks