## Slide 1
Stem Friction and Packing Stress Influence on the Sealing Behavior of Fugitive Emission Control Valves
CONFERENCE
ORGANIZERS

## Slide 2: Stem Friction and Packing Stress Influence on the Sealing Behavior of Fugitive Emission Control Valves
How to evaluate Control Valve packings performance and what is the friction role in these products?
Carlos D. Girão | Technical Director at Teadit

## Slide 3: Agenda
Main Fugitive Emissions (FE) Standards
Fugitive Emissions (FE) Packings
Friction Test
Fugitive Emissions Testing
High Temperature Performance
Preparing for the Future
Conclusion
CONFERENCE ORGANIZERS

## Slide 4: Main Fugitive Emissions Standards
624
641
622
API
15848-1
15848-2
ISO
Packing Test
Valve Test
Multi-Turn
Valve Test
Quarter-Turn
Valve Test
Multi & Quarter
Valve Test
Quality Control
API 641 and ISO 15848-1 are the most required test for Control Valves

## Slide 5: Main FE Standards
API 641 2nd Ed. (Isolating Valve)
ISO 15848-1:2015 CC (Control Valves)
Thermal Cycles: 3 (260°C)
Mechanical Cycles: 610
Test Media: Methane
Max. Leakage: 100 ppm
Thermal Cycles: 2, 3 or 4 (User Temp)
Mechanical Cycles: 20k, 40k or 100k
Test Media: Methane or Helium
Allowable Leakage Tiers:
  50, 100, 500 ppm (for Methane)

## Slide 6: Fugitive Emissions Packings
CONFERENCE ORGANIZERS
ORGANIZERS
Flexible Graphite
Metallic Alloy Jacket
PTFE Coating

## Slide 7: Fugitive Emissions Packings
Why is PTFE used in FE Packings?
ASTM¹, Shell² and API³ either limit PTFE content or have specific procedures for it.
  Is friction reduction significant?
  Is it necessary for FE service?
¹ASTM F2191 ²Shell SPE 85/204 ³API 622 3rd Ed

## Slide 8: Fugitive Emissions Packings
STYLE | DESCRIPTION | TYPICAL APPLICATION | 
A | Flexible Graphite with a Nickel-Chrome wire reinforcement jacket. | Applications with higher temperatures, high pressure condensed steam | 
B | Flexible Graphite with a Nickel-Chrome wire reinforcement jacket, coated with PTFE Lubricant (less than 10%). | Premium packing for API622 requirements | 
C | Flexible Graphite with PTFE thread embedded with tracer particles reinforcement jacket. No additional coating | Premium packing for Control Valve Service | 
Packings Description

## Slide 9: Control Valve Test Rig
Valve Size: 2’’ 300#
Packing Size: ¼’’ (6,4mm)
Thermocouple – Packing Gland
Thermocouple – Valve Body
Thermocouple – Valve Flange
Load Sensing Studs – 1 & 2
1
2
3
4
1
2
3
4
4

## Slide 10: Friction Test Procedure
Pre-load (1 MPa) is applied individually to each ring to accommodate the packing;
A total of 5 rings are installed;
The desired test load is applied;
Packing is allowed to dwell for 3 minutes;
The desired test load is re-applied;
Valve performs one complete mechanical cycle;
Test evolves to next stress stage and steps 3-7 are executed again.

## Slide 11: Friction Test Results
Room Temperature
Style A
No PTFE
Flex Grap.
Ni-Cr Mesh
Style B
<10% PTFE
Flex Grap.
Ni-Cr Mesh
Style C
Flex Grap.
PTFE Mesh

## Slide 12: Friction Test Results
High Temperature (260°C)
Style A
No PTFE
Flex Grap.
Ni-Cr Mesh
Style B
<10% PTFE
Flex Grap.
Ni-Cr Mesh
Style C
Flex Grap.
PTFE Mesh

## Slide 13: ISO 15848-1 FE Test
Test Procedure
2 thermal cycles (260°C)
20 000 mechanical cycles
  Stroke: 50% ± 10%
  Speed: 2 mm/sec
Media pressure: 40 bar (Methane)
Packing Stress: 60 MPa (5 rings)
Leakage measurements with sniffer

## Slide 14: ISO 15848-1 FE Test
Test Results – Style A
Style A
No PTFE
Flex Grap.
Ni-Cr Mesh
Min. Packing Stress: 22 Mpa (S-9)
Max. Packing Stress: 60 Mpa (S-1)
Max. Leakage: 142 ppm (S-9)
Average Leakage: 38 ppm
ISO FE CM – CC1 – SSA 0 – t200°C

## Slide 15: ISO 15848-1 FE Test
Test Results – Style B
Min. Packing Stress: 31 Mpa (S-9)
Max. Packing Stress: 60 Mpa (S-1)
Max. Leakage: 2 ppm (S-9)
Average Leakage: 0.62 ppm
ISO FE AM – CC1 – SSA 0 – t200°C
Style B
<10% PTFE
Flex Grap.
Ni-Cr Mesh

## Slide 16: ISO 15848-1 FE Test
Test Results – Style C
Min. Packing Stress: 32 Mpa (S-9)
Max. Packing Stress: 60 Mpa (S-1)
Max. Leakage: 4.2 ppm (S-3)
Average Leakage: 0.56 ppm
ISO FE AM – CC1 – SSA 0 – t200°C
Style C
Flex Grap.
PTFE Mesh
1
2
3
4
5
6
7
8
9

## Slide 17: How much can the right sealing solution reduce fugitive emissions?
CONFERENCE ORGANIZERS
ORGANIZERS
How to calculate leakage losses???

## Slide 18
29% Industry
20% Agro
18% Building
16% Transportation
6% Fugitive Emission
3% Waste
8% Otthers

## Slide 19
Considering a small refinery
5,000 Valves
Leakage Estimation:
0.0268 x 24h x 365d x 5,000 =
= 1,173,840kg
Aprox. 1,200 Ton/yr
What dos EPA say?
If you do NOT measure...

## Slide 20
Considering a small refinery
5,000 Valves
Leakage Estimation:
2.29*10-6 x (0.56ppm)0,746 x 24h x 365d x 5,000=
= 65kg
Less than 100 kg/yr
What dos EPA say?
If you DO measure... and use a premium product

## Slide 21
Test show that PTFE improves fugitive emissions performance, specially in Control Valves. Adding a controlled, small amount of PTFE will:
  Lower stem friction;
  Reduce packing wear;
  Decreases packing relaxation.
Packing Stem Friction is heavily benefited from PTFE addition in packings:
  Up to 40% less friction at ambient temperature;
  This effect is increased with higher temperatures.
The selection of the RIGHT packings can have a considerable positive impact on the reduction of GHG
  Based on EPA correlation factors there is a reduction of up to 1,100 Ton/yr of emissions considering a small refinery
Final Remarks

## Slide 22
Carlos D. Girão | Technical Director at Teadit
carlos.girao@teadit.com
João H. Pontes | R&D Specialist at Teadit
joao.pontes@teadit.com

## Slide 23
ORGANIZING SECRETARIAT
Ph. +39 035 3230904
e-mail info@industrialvalvesummit.com
www.industrialvalvesummit.com
CONFERENCE ORGANIZERS
Ph. +39 3474908420
e-mail segreteria@valvecampus.com
www.valvecampus.com
Thanks