## Slide 1: Apuzzo Francesco
The new regulatory framework of the Low Emission Graphite Packings for Industrial Valves
R&D Manager – Carrara Spa
ORGANIZERS
SCIENTIFIC COMMITTEE
IVS 2022
Technical Conference

## Slide 2
Biography
I’m a Mechanical Engineer graduated to the MIP Politecnico of Milan. I am CTO of Carrara SpA, managing the R&D and the Technical Department, and President of VALVEcampus, the Association of Manufacturers of Industrial Valves and Components for the Oil & Gas and Power Industries cooperating with the international exhibition IVS Industrial Valve Summit. I’m 27 years experienced in industrial sealing systems especially in the field of the stem sealing for industrial valves about which I published many technical papers.

## Slide 3
The new regulatory framework of the low emission graphite packings for industrial valves
The fighting for reducing the fugitive emissions is still worldwide a priority objective both for the Valve Manufacturers and for their Clients.
All countries have issued national regulations both for the New Equipment take-over (Valves certified LE) and for their yearly (half-yearly, quarterly) control with the LDAR - Leak Detection And Repair program.
About the New Equipment, the prototype and production FE test, following many years where the regulatory framework was frozen today some relevant news have been introduced drawing a new paradigma for the graphite stem packings.
ISO 15848
VDI 2440
API std 622 & 624(641)
IOGP
TQ39 FE Approach

## Slide 4
TA - Luft issued a new national regulatory framework adopting the std ISO15848 for industrial valves therefore the VDI2440 doesn't is anymore in place.
It is an important change of POV since the VDI2440 test was a stem packing test performed with a fixture while the ISO15848 test qualifies the valve together with the gasket (integrated system).
Note that the FE ISO15848 qualify the Performance Class of the valves on the basis of three criteria:
Tightening Class
Endurance Class
Temperature Class
ISO 15848
VDI 2440
Performance Class
The new regulatory framework of the low emission graphite packings for industrial valves

## Slide 5
About the API, which tests the stem packing, the API std 622 has been modified including a supplementary FE test while the API std 624(641) remained unchanged.
Also in this case it is an important paradigm shift since an additional FE test at 400 °C has been added together more stringent requirements regarding the raw materials, the limitation of PTFE and wet lubricants, the weight loss test.
API std 622 & 624 (641)
Unchanged
Limitated PTFE & Wet Lubricants Content
Packing Weight Loss Test
Raw Material TGA Test
Supplementary FE Test at 400°C
The new regulatory framework of the low emission graphite packings for industrial valves

## Slide 6
The new regulatory framework of the low emission graphite packings for industrial valves
The TGA test analyzes the oxidative trend of the product. The test can be conducted in accordance with the std EN 14772 or in accordance to the std FSA-G-604-07 A(B).
For both, the acceptance criteria requires a cumulative oxidation within predetermined limits.
The execution of these tests both on the raw materials and the finished products (die-formed and braided packing rings) aims to measure the quality of the graphite and the content of Wet Lubricants.

## Slide 7
The IOGP S-562 “Supplementary Requirements to API Specification 6D Ball Valves” and S-611 “Supplementary Requirements to API 600 Steel Gate Valves and to API 603 CRA Gate Valves” require for the graphite stem packings the compliance with the main international FE standards included the limitations to the detrimental materials and the weight loss of the materials at high temperature.
IOGP
S-562
S-511
ASTM F2168 / F2191
API std 622
ISO15848
The new regulatory framework of the low emission graphite packings for industrial valves

## Slide 8
The approach called TQ39 introduce new correlation between oxidation rate (of the graphite), temperature service °C and service life.
This approach is based on several criteria that if implemented in the equation provided by ASME can predict the suitable service temperature for complying the oxidation rate of the graphite calculated by TGA test at 670°C or viceversa (if it is set the temperature it is predicted the acceptable oxidation rate).
How long has to work the graphite packing (ex. 50.000 hours)?
What is it the temperature for this period of time (ex. 408°C)
Apply the equation and calculate the acceptable oxidation rate and compare the result with the TGA oxidation rate.
TQ39
ASME PVP-2017-65027
The new regulatory framework of the low emission graphite packings for industrial valves

## Slide 9
The new regulatory frame work about the LE graphite packings for industrial valves lead toward a new generation of stem packings engineered for meeting both the FE criteria and the long life service which can be guaranteed by the low oxidation rate and by limited content of PTFE and other detrimental materials for reducing the stem corrosion’s risk. For achieving these goals the packings shall be manufactured with graphite rich of inhibitor of oxidation
CONCLUSION
The new regulatory framework of the low emission graphite packings for industrial valves

## Slide 10: Q & A SESSION
ORGANIZERS
SCIENTIFIC COMMITTEE
Thank you for your attention!
IVS 2022
Technical Conference